École des Vergers — Specification extract, section K10

Plasterboard linings and partitions

K10/110 Metal stud partition, 100 mm

Studs: galvanised steel C stud at 600 mm centres, 92 mm, to the head and floor channels specified. Deflection head to be provided where the partition abuts a concrete soffit.

Linings: two layers of 12.5 mm plasterboard each side, joints staggered. Fire rating EI30 where scheduled. Tapered edge boards, jointed and filled ready for decoration.

Insulation: 75 mm mineral wool, density 45 kg/m3, friction fitted between studs. Full fill, no gaps at the head or at service penetrations.

Acoustic performance: minimum Rw 47 dB where the partition separates a classroom from a corridor. Test evidence for the exact build-up to be provided before installation.

K10/120 Service penetrations

All penetrations through fire-rated partitions to be sealed with a proprietary system tested in the same build-up. Sleeves, collars and batts to be recorded on the fire stopping register with a photograph of each before the lining is closed.

K10/130 Junctions

Partitions to be continuous to the soffit where the fire or acoustic rating requires it. Partitions stopping at ceiling level are permitted only where scheduled as non-rated. Where a partition abuts glazing, a flexible closer is to be used, not a rigid bead.

K10/140 Tolerances

Plumb within 3 mm in 2 400 mm. Flatness within 3 mm under a 1 800 mm straight edge. Board joints not to coincide with door openings.